## Slide 1: Computational modeling of refractory metals and alloys
Bochuan Sun
Materials Science and Engineering, Clemson University
PhD Qualifying Exam
ODTT

## Slide 2: Dissertation research objectives
Thrust 2: Design and Develop a Novel Tungsten-Based High-Entropy Alloy
Thrust 1: Study the irradiation effects in pure tungsten
Strain Effects on the Diffusion Properties of Near-Surface Self-Interstitial Atoms (SIAs) and Adatoms in Tungsten
Rate of Edge Dislocation Escape from a Void in Tungsten
Mobility of Screw Dislocation after Absorbing Vacancies/SIAs

## Slide 3
Introduction
Introduce plasma-facing materials (PFM)
Difficulties in PFMs
Background
Irradiation damage in body-centered cubic (BCC) tungsten (W)
Formation of fuzz structure
Core effects of high-entropy alloys (HEA)
Simulation methodologies
Strain Effects on the Diffusion Properties of Near-Surface Self-Interstitial Atoms (SIAs) and Adatoms in Tungsten (Finished)
Study the vacancy diffusion mechanism in the dislocation core
  Preliminary Results: Rate of edge dislocation escape from a void in BCC tungsten
Mobility of screw dislocation after absorbing vacancies/SIAs
Design and develop a novel tungsten-based refractory high-entropy alloy
Research Plan & Preliminary Results

## Slide 4: Structural Reliability under Irradiation Damage
Fusion reaction:
D : deuterium
T : tritium
n : neutron
Divertor
Irradiation hardening
Irradiation embrittlement
Irradiation swelling
Irradiation creep
Tokamak fusion reactor (International Thermonuclear Experimental Reactor (ITER)) [1]
[1] The beauty of the beast. ITER 2013. http://www.iter.org/newsline/252/1449. Accessed 13 Dec 2020
Tungsten (W) is a common plasma-facing material (PFM) because of:
high sputtering threshold
high thermal conductivity
high melting point
low sputtering yield

## Slide 5: Irradiation damage in body-centered cubic (BCC) tungsten (W)
SEM pictures of fuzz structure in W
[1] Wirth, B. D., et al. "Fusion materials modeling: Challenges and opportunities." MRS bulletin 36.3 (2011): 216-222.
[Kajita S, Sakaguchi W, 2009]
[Baldwin M.J., Doerner R.P., 2009]
Schematics of the effect of irradiation on the atomic structure in tungsten [1]

## Slide 6: Formation of fuzz structure
Schematics of initial fuzz growth from TEM images[1]
[1] Kajita, Shin, et al. "TEM observation of the growth process of helium nanobubbles on tungsten: Nanostructure formation mechanism." Journal of nuclear materials 418.1-3 (2011): 152-158.
[2] Dasgupta, Dwaipayan, et al. "On the origin of ‘fuzz’ formation in plasma-facing materials." Nuclear Fusion 59.8 (2019): 086057.
Schematic representation of the evolution of surface nanostructure[2]
Mechanism:
Helium (He) atoms deposit in W
He atoms encounter other He atoms and form bubbles
Large He bubbles can eject W atoms to bulk to become self-interstitial atoms (SIAs)
W SIAs can form prismatic <111>-dislocation loops and annihilate on the surface, making a flat surface wavelike.
Near-surface He bubbles break and leave craters.

## Slide 7: Considerations for Utilizing Tungsten
Disadvantages
Very low fracture toughness
Blistering (<800 K); He bubbles (1250 -1600 K)
Fuzz formation
High Ductile-to-brittle transition temperature
Low oxidation resistance
Advantages
High sputtering threshold
High thermal conductivity
High melting point
Low sputtering yield
Good High-temperature strength

## Slide 8: Advantages of HEA
Element | Tm (K) | Atomic Radius ()
Cr | 2180 | 1.28
V | 2163 | 1.34
W | 3683 | 1.39
Ta | 3269 | 1.49
Hf | 2500 | 1.59
Element | Tm (K) | 
Cr | 2180 | 1.28
V | 2163 | 1.34
W | 3683 | 1.39
Ta | 3269 | 1.49
Hf | 2500 | 1.59
[1] O. El-Atwani, N. Li, M. Li, A. Devaraj, J. Baldwin, M.M. Schneider, D. Sobieraj, J.S. Wróbel, D. Nguyen-Manh, S.A. Maloy, E. Martinez, Outstanding radiation resistance of tungsten-based high-entropy alloys, Science advances 5(3) (2019) eaav2002.
W-Ta pairs suppress He bubble formation.
V increases the recombination of Frenkel pairs
Hf is used to increase the ductility
Single solid-solution phase at a high temperature
No loops were shown to form
Hardness remains after irradiation
Order-disorder transition temperature of this composition is high
Preliminary data of W38Ta36Cr15V11 [1]
(b)
Multiple principles element
Single solid solution phase
Notes: Move preliminary results to the background

## Slide 9: Design of Materials with Optimized Properties – High-Entropy Alloys
High entropy
Lattice distortion
Modified diffusion
Cocktail
4 core effects
W15Ta35V15Cr35
2000 K

## Slide 10: High entropy and lattice distortion effect
High entropy effect
Lattice distortion effect
500 K
2000 K
W15Ta35V15Cr35
Random configurational entropy of mixing:
Atomic size mismatch:
Lattice distortion:
Gibbs free energy:
Atomic size mismatch versus lattice distortion [1]
[1] Song, Hongquan, et al. "Local lattice distortion in high-entropy alloys." Physical Review Materials 1.2 (2017): 023404.

## Slide 11: Modified diffusion effect in HEAs
[1] Pickering, E. J., and N. G. Jones. "High-entropy alloys: a critical assessment of their founding principles and future prospects." International Materials Reviews 61.3 (2016): 183-202.
[2] Tsai, K-Y., M-H. Tsai, and J-W. Yeh. "Sluggish diffusion in co–cr–fe–mn–ni high-entropy alloys." Acta Materialia 61.13 (2013): 4887-4897.
Schematic representation of sluggish diffusion effect [1]
Energy barrier to migrating Ni in different matrices [2]
The sites with lower potential energy for an element would become atomic traps and increase the energy barrier and the activation energy for diffusion

## Slide 12: Utilizing the Cocktail effect
The properties of HEAs relate to the properties of its composing element (not linear).
Yield strength as function of Sc content in Sc-containing (FeCoNi)1−xAlx [1]
[1] Rui, Z. H. O. U., et al. "Effect of Al and Sc on deformation behavior of FeCoNi multi-element alloys." Transactions of Nonferrous Metals Society of China 29.10 (2019): 2109-2116.

## Slide 13: Modeling Materials at the Atomic Scale
Cluster expansion (CE)
[1] Durrant, Jacob D., and J. Andrew McCammon. "Molecular dynamics simulations and drug discovery." BMC biology 9.1 (2011): 1-9.
m: multiplicity
J: the concentration independent effective cluster interaction (eci)
the average correlation funcion
First principal calculations (DFT)
Cluster expansion
Fit eci based on DFT results
Monte Carlo simulations
Thermal properties
Equilibrium properties of many-body system
Density functional theory (DFT)
The ground-state electron density uniquely determines the electronic wavefunction.
The energy of an electron distribution can be described as a functional of the electron density, and this functional is a minimum ground-state density.
Kinetic
Interaction potential
External potential
Universal
Ground-state energy and elastic modulus
Molecular dynamics (MD) [1]
Initial atomic model
Calculate molecular forces acting on each atom
Move each atom according to those forces
Advance simulation time
Trajectories of atoms

## Slide 14: Focus of my dissertation work is divided into two thrust areas
Study the irradiation effects in pure tungsten
(3 projects)
Design and develop a novel tungsten-based high-entropy alloy
(1 project)
Study the irradiation effects in tungsten-based high-entropy alloys
In this dissertation
Science that will be enabled by this dissertation
part of the database for machine learning
Provide methodologies

## Slide 15: Project 1: Strain Effects on the Diffusion Properties of Near-Surface Self-Interstitial Atoms and Adatoms in Tungsten
Experimental approach
Lammps codes
>10k atoms
Temperature range: 700K to 1400K
Strain range: -0.008 to 0.008
Mechanism (known):
Helium (He) atoms implant in W
He atoms encounter other He atoms and form bubbles
Large He bubbles can eject W atoms to bulk to become self-interstitial atoms (SIAs)
W SIAs can agglomerate into prismatic <111>-dislocation loops and annihilate on the surface, making a flat surface wavelike.
Near-surface He bubbles break and leave craters.
Strain effect (unknown)

## Slide 16: Methodologies for Project 1
3 sets of MD simulations are performed by Lammps codes and visualized by using OVITO.
Set 1:
SIA added to the center of the bulk and diffuses to the surface
Simulation supercell size: 61.5 × 76.1 × 86.6 Å3
Different temperatures: 700 K, 850 K, 1000 K
Different biaxial strain: -0.007 to 0.007
Target: Diffusivity of SIA inside bulk at different temperatures and strains
5 independent simulations for each set of parameters
Orientation: , ,
Set 2:
SIA is added to the surface of the bulk and migrates on the surface
Simulation supercell size: 61.5 × 76.1 × 86.6 Å3
Different temperatures: 1000 K to 1400 K
Different biaxial strain: -0.008 to 0.008
Target: Diffusivity of SIA on surface at different temperatures and strains
5 independent simulations for each set of parameters
Set 3:
Add a SIA to the bulk randomly Every 200 ps
Simulation supercell size: 123.0 × 152.2 × 86.6 Å3
Temperature: 1000 K
Different biaxial strain: -0.008 to 0.008
Target: morphological evolution on urface
: the most probable time for a diffusing particle to reach a point in space from a given origin in 1D
: the travel distance of SIAs (4.4 nm in this simulation)
: diffusivity of SIA
: jumping distance
: diffuse rate
: activation stress
: applied stress tensor
: atomic volume
SR: surface roughness
: average height

## Slide 17: Preliminary Results of Project 1
SIA in the center of the bulk
SIA on the surface
Surface morphology changes
New knowledge generated during Project 1:
Compressive strain increases the diffusivity of the SIA
High temperature increases the diffusivity
Effect of strain on morphology change is complicated, not only depending on the strain but also the number of SIAs

## Slide 18: Project 2: Understanding the Rate of Edge Dislocation Escape from a Void in bcc Tungsten
Irradiation introduces vacancies in the W bulk.
Vacancies accumulate and form voids which are obstacles to dislocation gliding and contribute to hardening.
Edge dislocation pinned by a void and breakthrough under stress [1]
Superjog on a dislocation line after it was released from the 6 nm void in W [2]
[1] Osetsky, Y.N. Atomic-scale mechanisms of void strengthening in tungsten. Tungsten 3, 65–71 (2021).
[2] P. Yu, G Liu, K. Wu, Y. Cui, G. Zhao, Y. Shen, Exploring the effects of the sheared voids on the hardening of tungsten using atomistic simulations, J. Nucl. Mater. 562 (2022) 153548.
Previous research has revealed:
How does absorption contribute to irradiation hardening?
Notes: Time and rate of escape is unknown and that’s what I contribute to the science, to make the simulation about the irradiation hardening more accurate

## Slide 19: Methodology for Project 2
Radius of void(nm) /number of vacancies in void | Temperature (K) |  |  |  |  |  | 
0.22/ 3 vacancies | 1000 | 1100 | 1200 | 1300 | 1400 |  | 
0.3/ 5 vacancies | 1000 | 1100 | 1200 | 1300 | 1400 |  | 
0.335/ 10 vacancies | 1200 | 1300 | 1400 | 1500 | 1600 |  | 
0.35/ 13 vacancies | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000
0.38/ 15 vacancies | 1600 | 1700 | 1800 | 1900 | 2000 |  | 
0.4/ 20 vacancies | 1800 | 1900 | 2000 | 2100 | 2200 |  | 
0.5/ 34 vacancies | 2000 | 2100 | 2200 | 2300 | 2400 |  | 
0.6/ 58 vacancies | 2000 | 2100 | 2200 | 2300 | 2400 |  | 
MD simulations will be done using LAMMPS codes
Simulation details:
  BCC system
  Orientation: [ 1 1], [1 0], [1 1 2]
  Edge dislocation with Burgers vector [-1 1 1] is placed in the center of the system with the dislocation tangent to the z-direction
  A spherical cluster of atoms is deleted to form a void at the center of the dislocation line
  Radius of the void and temperature are 2 key parameters in this project
  5 independent simulations for each set of parameters
No stress

## Slide 20
Methodology for Project 2
2 escaping mechanisms: Fully absorb & partially absorb
We account for the number of steps between the first step and the step when the void has been fully absorbed or there is no interaction between dislocation and void.
Number of steps Simulation time Escaping rate

## Slide 21: Project 2 Preliminary Results Understanding the Rate of Edge Dislocation Escape from a Void in bcc Tungsten
a = 0.59 -1ps-1, b = ps-1, c = 0.28 (eV/) , and d = -0.03 (eV)
R2 = 0.723
Escaping rate of different void sizes and at different temperatures

## Slide 22: Next Step for Project 2 Understanding the Rate of Edge Dislocation Escape from a Void in bcc Tungsten
Chart: Reaction coordinate
| 0 | 7.1420436000000004E-2 | 0.14284177000000001 | 0.21426545999999999 | 0.28569319999999998 | 0.35712480000000002 | 0.42855786000000001 | 0.49999084999999999 | 0.57142822999999998 | 0.64286823000000004 | 0.71430808999999995 | 0.78574516999999999 | 0.85717016999999995 | 0.92858664000000002 | 1 | 1.07141336 | 1.1428298300000002 | 1.21425483 | 1.2856919100000002 | 1.3571317700000001 | 1.42857177 | 1.5000091499999999 | 1.57144214 | 1.6428752 | 1.7143068000000001 | 1.78573454 | 1.85715823 | 1.9285795640000001 | 2 | 2.0714133600000002 | 2.1428298300000002 | 2.2142548299999998 | 2.2856919100000002 | 2.3571317700000001 | 2.42857177 | 2.5000091499999999 | 2.5714421399999998 | 2.6428751999999998 | 2.7143068000000001 | 2.78573454 | 2.85715823 | 2.9285795640000001 | 3
 | 0 | -0.0031161 | 0.0058539 | 0.028585 | 0.054779 | 0.11373 | 0.097273 | -1.6317 | -1.7396 | -1.8088 | -1.8736 | -2.1292 | -2.1572 | -2.1682 | -2.1627 | -2.1744 | -2.1778 | -2.1184 | -2.1129 | -2.1177 | -2.1032 | -2.0215 | -1.5035 | -0.75491 | -0.13255 | 0.075222 | -0.3341 | -0.67108 | -0.6745 | -0.67195 | -0.63098 | -0.5588 | -0.45892 | -0.35268 | 1.1561 | 1.1621 | 0.19001 | 0.12207 | 0.077141 | 0.046325 | 0.01652 | -0.00027743 | 1.9092e-07
Result of the pathway ‘1 2 3’
Finishing the map of activation energy for each pathway
The analysis of the potential energy landscape for a vacancy to diffuse when located near a dislocation jog

## Slide 23: Project 3: Mobility of screw dislocation after absorbing vacancies/SIAs
Hirth, John Price, Jens Lothe, and T. Mura. "Theory of dislocations." Journal of Applied Mechanics 50.2 (1983): 476.
Pure screw dislocation containing jogs of both signs
When helical dislocation climbs, the center of the helical turn may change
Jogs absorb vacancies
Move perpendicular to screw dislocation in a direction determined by the sign of the jogs
All segments have developed some edge components
Sign of edge components differ
Absorb vacancies and climb in different directions normal to paper.

## Slide 24: Methodology for Project 3
The number of atoms: >200,000
Lammps code
Initial configuration
Add a ½ <1 1 1> screw dislocation at the center
Uniformly add 10 W-SIAs or vacancies on the dislocation line
Relax the system
Add strain and calculate the mobility of the dislocation
100 SIAs or vacancies?
Y
N

## Slide 25: Preliminary results and next steps for Project 3
Next steps:
add stress
calculate the mobility of helical dislocation
SIAs absorbed by a screw dislocation
Potential energy (eV)
Vacancies absorbed by a screw dislocation
Potential energy (eV)
Small void

## Slide 26: Project 4: Calculate the order-disorder transition temperature and elastic response of different compositions of the W-based refractory HEA
Chart: Cr25Ta25W25V25
500 K
2000 K
SRO parameter:
is the pair probability of elements i and j
is the concentration of element i
Average of 1st and 2nd nearest neighbor (bcc):
[1] Sobieraj, Damian, et al. "Chemical short-range order in derivative Cr–Ta–Ti–V–W high entropy alloys from the first-principles thermodynamic study." Physical Chemistry Chemical Physics 22.41 (2020): 23929-23951.
[1]
bcc structure
Cluster Expansion + Metropolis Monte Carlo
Notes: Add SRO equation

## Slide 27: Research Plan for Project 4 Short-range order (SRO)
Smix and Hmix of equiatomic Cr-Ta-W-V HEA
Instead of random configurational Smix, we calculate from specific heat.
By combining the inflection point in the enthalpy of mixing and the short-range order figure, we find the ODTT

## Slide 28: Project 4 Research Plan Develop quaternary phase diagrams for Cr-Ta-V-W HEA
The contribution of TSmix and Hmix in the whole range of compositions at different temperatures of Fe-Cr-Mn-Ni alloy [1]
[1] Fedorov, Mark, et al. "Phase stability and magnetic properties in fcc Fe-Cr-Mn-Ni alloys from first-principles modeling." Physical Review B 101.17 (2020): 174416.
Free energy of mixing at 1000 K
ODTT
ODTT: inflection point on the enthalpy of mixing versus temperature
Chart: Cr25Ta25W25V25

## Slide 29: Project 4 Research Plan Develop quaternary phase diagrams for Cr-Ta-V-W HEA
Common tangent on Gibbs free energy [1]
[1] Porter, David A., Kenneth E. Easterling, and Mohamed Y. Sherif. Phase transformations in metals and alloys. CRC press, 2021.
Compute the phase diagram of pseudo binaries, like: Crx(TaVW)1-x.
Compute the quaternary phase diagram of different bcc phases, like: α and αʹ. They have the same crystal structure, but the clusters are different.
Compute the quaternary phase diagram of bcc and fcc structure.

## Slide 30: Contribution to this project and broader impacts for science
Study the irradiation effects in pure tungsten
Design and develop a novel tungsten-based high-entropy alloy
Study the irradiation effects in tungsten-based high-entropy alloys
In this dissertation
Science that will be enabled by this dissertation
part of the database for machine learning
Provide methodologies

## Slide 31: Acknowledgements
MUEXLY Group
Dr. Enrique Martinez Saez
Dr. Qianran Yu
Hyunsoo Lee
Liam Myhill
Sanad Alturk
Mohammad Hossein Nahavandian
Muhammed Kose
Jacob Jeffries
Prashant Kumar Jha
Akshay Korpe
Committee members
Dr. Marian Kennedy
Dr. Dilpuneet Aidhy
Dr. Jianhua Tong
Dr. John Ballato
Clemson MSE staff
Diane Nations Swope
Tonya Bledsoe
Laura Kinard
David White
James Lowe
My wife: Sha Wan (But she is too shy…)

## Slide 32: Questions and discussion
ODTT
Project 3
Project 2
Project 1
Project 4

## Slide 33: Elastic properties
Backup
Instead of enthalpy of mixing, we can also fit the new concentration-independent effective cluster interaction J of elastic constant C11, C12, and C44. Then using the same correlation function obtained by applying Monte Carlo to calculate the elastic constant and the elastic modulus.